Ultra-Fast Machine Learned Interatomic Potential for MoS₂ Enabling Non-Equilibrium Molecular-Dynamics Simulation of Epitaxial Growth

Emir Bilgili1*, Nicholas Taormina1, Richard Hennig2, Simon R. Phillpot2, Youping Chen1

1 Department of Mechanical and Aerospace Engineering, University of Florida, Gainesville FL 32611

2 Department of Materials Science and Engineering, University of Florida, Gainesville FL 32611

SI Table I. Energetics of Defect Structures in Monolayer MoS2: DFT vs UF3

| Defect Structure | N atoms | DFT Energy (eV) | DFT ΔEdefect (eV) | DFT ΔEdefect% (%) | UF3 Energy (eV) | UF3 ΔEdefect (eV) | UF3 ΔEdefect% (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pristine Monolayer | 75 | -558.7 | 0.0 | 0.0 | -126.1 | 0.0 | 0.0 |
| VS | 74 | -539.3 | 19.3 | 3.6 | -122.4 | 3.7 | 2.9 |
| MoS₂ | 74 | -536.2 | 22.5 | 4.2 | -118.3 | 7.8 | 6.2 |
| S₂Mo | 76 | -534.3 | 24.4 | 4.6 | -120.1 | 5.9 | 4.7 |
| VS₂ | 73 | -532.4 | 26.2 | 4.9 | -118.8 | 7.3 | 5.8 |
| VSVS | 73 | -532.3 | 26.3 | 4.9 | -118.7 | 7.3 | 5.8 |
| VMo | 74 | -527.9 | 30.7 | 5.8 | -121.3 | 4.8 | 3.8 |
| Schottky_ VS₂ | 72 | -514.6 | 44.1 | 8.6 | -114.0 | 12.0 | 9.5 |
| VMoS₃ | 71 | -512.3 | 46.3 | 9.0 | -113.5 | 12.6 | 10.0 |
| VMoS₆ | 68 | -492.6 | 66.0 | 13.4 | -105.5 | 20.6 | 16.3 |